## Slide 1: Hydrazine Adsorption Conformations on metal surfaces
Mohammad Kemal Agusta, Wilson. A. Dino, Hiroshi Nakanishi, Hideaki Kasai
Graduate School of Engineering
Osaka University

## Slide 2
Motivations:
Hydrazine adsorption on metal surface could serve as model for adsorption which involves lone-pair and conformational transformation.
The adsorption process yields conformations dependent type structures which gives more complex reaction pahtways but also open possibility of controlling molecular structure on surfaces.
Hydrazine adsorption and reaction phenomena can be found in various important technologies such as fuel-cell, chemical industries and also play important role in as reduction agent in the synthesize of nano particle
Methods:
Theoretical approach based on Density Functional Theory. GGA – PBE for exchange-correlation functional, plane-wave basis set, Projector Augmented Wave (PAW) as implemented in VASP.
Calculation were done for adsorption on Ni(111), Cu(111), Co(0001), Pd(111) and Pt(111)

## Slide 3
Hydrazine molecule (N2H4):
NH2 – NH2 via N – N sigma-bond: internal rotation around N – N axis
Three critical conformations: gauche, anti and cis
Gauche-conformation as the most stable conformation in the gas-phase
Gas-phase
Adsorbed-phase
Adsorption configuration for each respective conformations, found in most metal surfaces.
Hydrazine prefers top-site, bonded through its N atom
gauche
anti
cis

## Slide 4
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Eads (eV)
Chart: 
| Co(0001) | Ni(111) | Cu(111) | Pd(111) | Pt(111)
anti | -0.65 | -0.61 | -0.35 | -0.73 | -1.02
gauche | -0.59 | -0.58 | -0.36 | -0.65 | -0.87
cis | -0.26 | -0.15 | 0.16 | -0.12 | -0.23
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Eads (eV)
Chart: 
| Co(0001) | Ni(111) | Cu(111) | Pd(111) | Pt(111)
anti | -0.94 | -0.82 | -0.53 | -1.05 | -1.48
gauche | -0.92 | -0.7 | -0.46 | -0.92 | -1.21
cis | -0.79 | -0.61 | -0.2 | -0.73 | -1.08
0.25 ML
0.11 ML
anti
gauche
cis
anti: most-stable conformation on surface
cis: least-stable conformation on surface
Coverage reduction  Stability increases  Repulsive interaction among adsorbate
Large permanent dipole-moment of cis-conformation (~3.11 debye) strong ads-ads repulsion
Eads = Esystem – Eclean surface - Ehydrazine
Trend of adsorption energy

## Slide 5
Stabilization mechanism of gauche-conformation in gas phase
14-electrons molecule, occupied anti-bonding HOMO  repulsion between the NH2 groupslone-pair repulsion
Gauche conformation stabilization:
Stabilization of HOMO (Walsh’s rule)
The anti-bonding character is reduced through mixing with N – H orbitalreduces lone-pair repulsion
The nearly degenerate of HOMO and HOMO-1 are fully occupied
HOMO
HOMO-1
HOMO
HOMO-1

## Slide 6
Stabilization mechanism of anti-conformation on surface
HOMO
HOMO-1
HOMO
HOMO-1
anti-bonding (AB)
bonding (B)
dative (D)
Projected LDOS of hydrazine/Ni(111)
Surface acts as a perturbation that removes the degeneracy in gauche-conformation (Jahn-Teller effect)
First-order charge transfer: between HOMO and dz2 orbital, derived states: AB (anti-bonding) and B (bonding). Charge transfer from anti-bonding orbital reduces repulsion  stabilizes anti-conformation & forms covalent bonding with the surface
Second-order charge transfer: HOMO-1 mix with HOMO through interaction with d-band. HOMO-1 polarized toward the surface  dative type of bonding with surface
AB
B
D
AB
B
D

## Slide 7
AB
B
D
AB
B
D
HOMO
HOMO-1
AB
B
D
The formation of strong chemisorption should always be accompanied by the conformation changes from gauche to anti.

## Slide 8
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
The mechanism is consistent for various surface materials
The differences in occupation of the anti-bonding orbital affects the stability of bonding and conformations.
Charge transfer (bonding formation) happens at the expense of conformational changes  gauche-conformation can be found in weak adsorption case such as on Cu(111)
Projected LDOS of hydrazine on several metal surfaces
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Eads (eV)
Chart: 
| Co(0001) | Ni(111) | Cu(111) | Pd(111) | Pt(111)
anti | -0.65 | -0.61 | -0.35 | -0.73 | -1.02
gauche | -0.59 | -0.58 | -0.36 | -0.65 | -0.87
cis | -0.26 | -0.15 | 0.16 | -0.12 | -0.23
anti
gauche
cis

## Slide 9
Experimental results:
XPS spectra of N(1s) of 0.5, 1 and 2 ML hydrazine on Pt(111) at 60 K.
Alberas et. al, Surf. Sci. 278 (1992) 51 - 61
on Pt(111) and Fe(111):
XPS results shows that hydrazine adsorbed on cis-conformation  one N(1s) peak indicates similar bonding environment for all N atoms.
The bonding with surface retains N – N bond, hydrazine decomposed through N – H bond cleaving
on Ni(111)
No information with regards to the structure. Decomposition products: N, H, NH, NH2, NH3, N2H2
Contradictions with theory:
DFT gives anti-conformation as the most stable structure
Adsorption stability in cis-conformation suffers from repulsive interaction among adsorbates.

## Slide 10
Ɛd - ƐF (eV)
Eads (eV)
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Chart: 
| -1.17 | -1.29 | -2.67 | -1.83 | -2.25
 | -0.65 | -0.61 | -0.35 | -0.73 | -1.02
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Eads (eV)
Chart: 
| Co(0001) | Ni(111) | Cu(111) | Pd(111) | Pt(111)
anti | -0.65 | -0.61 | -0.35 | -0.73 | -1.02
gauche | -0.59 | -0.58 | -0.36 | -0.65 | -0.87
cis | -0.26 | -0.15 | 0.16 | -0.12 | -0.23
The adsorption energy varies according anti-bonding states occupancy  can be correlated with
d-band center model : the higher position of d-band center with respect to the Fermi levellesser occupancy of anti-bonding statesstronger bonding, (with shorter N – N bond length )
Follows d-band center
Not follows d-band center, necessary to consider attraction/repulsion interaction proportional to coupling matrix element
Cu(111)
Pt(111)

## Slide 11
Approximation of Eads using Ehyb calculated based on perturbation model
d-states attractive
d-states repulsive
sp-states contribution
d-band extention
M – N distance obtain from DFT optimization
from LMTO description
Eads (eV)
Ehyb (eV)
Co(0001)
Ni(111)
Cu(111)
Pd(111)
Pt(111)
Chart: 
| -0.725215761020269 | -0.51154776003895 | -0.358262512869989 | -0.745702607177939 | -1.019525720657907
 | -0.65 | -0.61 | -0.35 | -0.73 | -1.02
α = 0.091
Esp = -0.60 eV

## Slide 12
 | anti | gauche | cis | Expa,b
Ni(111) N – N stretch NH2 rock N – M NH2 torsional Pd(111) N – N stretch NH2 rock N – M NH2 torsional Pt(111) N – N stretch NH2 rock N – M NH2 torsional | 1073 900 370 1046 903 376 1086 911 448 | 1095 838 349 1041 840 343 i103 1055 853 412 | 1061 850 308 i69 1053 849 262 i119 1059 843 319 45 | 1070 900 - - - - - - 1040 836 - -
Imaginary frequency is found at the lowest vibration mode of cis-conformation adsorption (except on Pt(111)))Transition state upon adsorbate decomposition
For the case of Pd(111), imaginary frequency also exists in gauche-conformation adsorptiontwo possibilities of decomposition pathways depend on conformation at transition states
The observed cis-conformation adsorption on experiments might be actually a transition state.
All experiments were done in a framework of studying decomposition pathways
a. Gland. et. al, Chem. Phys. Lett 119 (1985) 89
b. Alberas et. al, Surf. Sci. 278 (1992) 51 - 61
Vibrational modes (cm-1)

## Slide 13
Conclusions:
First-principle calculations based investigation has been done to clarify the mechanism of hydrazine adsorption on metal surfaces.
Hydrazine adsorbed on metal surfaces most stably on its anti-conformation, bonded through one of its N atom. Structure with gauche conformation is weaker than the one in anti-conformation. Cis-conformation is least stable configuration and a transition state. An exception is found for adsorption on Cu(111) where gauche is comparably stable to anti.
Interaction between the HOMO and HOMO-1 adsorbate orbital with the dz2 surface orbital play important role in stabilization of anti-conformation. The charge transfer shares the electron of HOMO to the surface, reducing the lone-pair repulsion and thus stabilize anti-conformation. The HOMO-1 is polarized to form a dative type of bonding to the surface.
The trend across a row in periodic table (Co(0001),Ni(111) and Cu(111)) follows the d-band center prediction. For the trend in a group in periodic table (Ni(111), Pd(111) and Pt(111) ) it is important to consider the repulsive/attractive interaction proportional to the coupling matrix element.