## Slide 1: 鉄系超伝導体における電子格子相互作用の 軌道揺らぎへの影響 Effect of electron-phonon interactions on orbital fluctuations in iron-based superconductors
野村悠祐、中村和磨A、有田亮太郎
東大工、九工大院A
新学術領域「コンピューティクスによる物質デザイン：複合相関と非平衡ダイナミクス」
計画班「第一原理有効模型と相関科学のフロンティア」
YN, K. Nakamura, and R. Arita, arXiv:1305.2995

## Slide 2: Ab initio downfolding for electron-phonon coupled systems
Low-energy models for electron-phonon coupled systems:
i,j: orbital (Wannier) indices (w): Wannier gauge s : spin index
O(p): the quantity with constraint (partially screened)
Q. How do we evaluate ?
A. Constrained random phase approximation (cRPA)
F. Aryasetiawan et al., Phys. Rev. B. 70 19514 (2004)

## Slide 3: Constrained RPA
exclude the contribution from
T↔T scattering
This screening process should be considered when we solve the low-energy effective model
・Independent particle polarizability(RPA)
F. Aryasetiawan et al., Phys. Rev. B. 70 19514 (2004)
V:virtual
T:target
EF
T
Occupied (O)
V
①
②
③
④
①
②
③
④
＝①＋②＋③＋④

## Slide 4: Ab initio downfolding for electron-phonon coupled systems
Low-energy models for electron-phonon coupled systems:
i,j: orbital (Wannier) indices (w): Wannier gauge s : spin index
O(p): the quantity with constraint (partially screened)
Q. How do we evaluate and ?
YN, K. Nakamura, and R. Arita, arXiv:1305.2995
cf. Desity-functional perturbation theory (without constraint)
S. Baroni et al, Rev. Mod. Phys. 73, 515 (2001).
A. Constrained density-functional perturbation theory

## Slide 5: Phonon frequency and electron-phonon coupling
Phonon frequencies and electron-phonon couplings are given by
(for simplicity we consider the case where there is one atom with mass M in the unit cell)
where
: characteristic
length scale
Dynamical matrix
E : electron ground-state energy
α: cartesian coordinates (x,y,z)
bare
Hartree + exchange correlation terms (screening)
Key quantity
ν：phonon mode
u : displacement of the ion
S. Baroni et al, Rev. Mod. Phys. 73, 515 (2001).

## Slide 6: Constrained density-functional perturbation theory
Partially screened quantities such as and
In the metallic case, is given by
exclude the target-target processes
n,m: band indices
V:virtual
T:target
EF
T
Occupied (O)
V
①
②
③
④
①
②
③
④
YN, K. Nakamura, and R. Arita, arXiv:1305.2995

## Slide 7: Iron-based superconductors
1111 system
111 system
122 system
11 system
Y. Kamiahara et al., J. Am Chem. Soc. 130, 3296 (2008).
G. R. Stewart, RMP 83, 1589 (2011).
I. R. Shein and A. L. Ivanovskii, Solid State Commun. 149,1860 (2009).
G. R. Stewart, RMP 83, 1589 (2011).
Z. Deng et al., Europhys. Lett. 87, 37004 (2009).
G. R. Stewart, RMP 83, 1589 (2011).
F.-C. Hsu et al., Proc. Natl. Acad. Sci. U.S.A. 105, 14262 (2008).
and more…

## Slide 8: Pairing symmetry: Iron pnictide
H. Kontani and S. Onari, PRL 104, 157001 (2010).
T. Saito et al., PRB 82, 144510 (2010).
Linearized Eliashberg equation:
f4
f3
f4
f3
Here spin and charge fluctuations are given by
and (within RPA)
Without el-ph interactions
χs > χc (spin fluctuations are dominant)
→ W < 0 (repulsive)
→ sign change in gap functions (s±-state)
χc > χs (charge fluctuations are dominant)
→ W > 0 (attractive)
→ no sign change (s++-state)
With el-ph interactions such that
Band structure
Fermi surfaces

## Slide 9
Spin fluctuations (enhanced by Hubbard U ) s±-wave
Orbital fluctuations (enhanced by el-ph interactions?) s++-wave
Q. Do el-ph interactions really enhance the orbital fluctuations?
Role of electron-phonon interactions

## Slide 10: Phonon-mediated interactions
Effective on-site el-el interactions coming from the exchange of phonons:
momentum-space average -> on-site quantity
We get
cf. (Kontani & Onari)
・ Jph is very small
・ not negligible compared to Coulomb repulsion U ~ 2 eV
・ these frequency dependent interactions vanish around ωl ~ ωD

## Slide 11: RPA analysis
T = 0.02 eV
n(filling) = 6.1
5-orbitals model
s±-wave state is realized
Gap functions in band representation
・ the magnitude of Jph is crucial to the enhancement of orbital fluctuations
・ spin fluctuations are dominant (since Jph is small in magnitude)

## Slide 12: Conclusion
developed a method for ab initio downfolding for el-ph coupled systems
Effective parameters for LaFeAsO:
    Uph(0) ~ U’ph(0) ~ -0.4 eV, Jph(0) ~ -0.02 eV
RPA analysis -> s± (due to the smallness of Jph )
YN, K. Nakamura, and R. Arita, arXiv:1305.2995