## Slide 1
野村悠祐、A中村和磨、有田亮太郎
東大工、A九工大院
フラーレン超伝導体の電子格子相互作用を含む低エネルギー模型導出
Ab initio derivation of low-energy model including phonon terms
for C60 superconductors
See also P29
改良された連続時間量子モンテカルロ法による
多軌道クラスター動的平均場理論
YN, S. Sakai, and R. Arita, arXiv: 1401.7488
YN-Nakamura-Arita, Phys. Rev. B 85, 155452 (2012)
YN, K. Nakamura, and R. Arita, Phys. Rev. Lett. 112, 027002 (2014)

## Slide 2: C60 superconductors
A15 system
Cs3C60 : Tc = 38K
fcc system
K3C60 : Tc=19K
Rb3C60 : Tc=29K
Cs3C60 : Tc=35K
O.Gunnarsson Rev.Mod.Phys. 69, 575 (1997)
Ganin et al, Nature 466,221(2010)
A.Ganin et al Nature Mater. 7,367-371(2008)
Y.Takabayashi et al Science 323,1285-1590(2009)
Phase diagram
Y. Ihara et al., EPL 94, 37007 (2011)
narrow band (molecular orbital + small hopping)
3band half-filling (LUMO)
Cs3C60 at ambient pressure: low-spin insulator (S=1/2)
Tc as a function of pressure shows dome-like behavior

## Slide 3: Superconductivity in C60 compounds
cf.
lattice parameter a
transfer integral t
band width W
density of states N(EF)
TC
can be explained within the BCS theory
old study
recent study
can not be explained within Migdal-Eliashberg theory
O.Gunnarsson Rev.Mod.Phys. 69, 575 (1997)
A15
fcc
Ganin et al, Nature 466,221(2010)
R. Akashi and R. Arita, PRB 88, 054510 (2013)
ωD~1000K

## Slide 4: Motivation
Q. What is the mechanism of superconductivity?
Q. Origin of low-spin state?
Q. Unified description of the phase diagram?

## Slide 5
EF
Target (T)
trace out
trace out
renormalize
Effective Hamiltonian
Ab initio Hamiltonian
global energy scale
low energy scale
Occupied (O)
Virtual (V)
Target (T)
Effective low-energy model

## Slide 6: Ab initio downfolding for electron-phonon coupled systems
Low-energy models for electron-phonon coupled systems:
i,j: orbital (Wannier) indices (w): Wannier gauge s : spin index
O(p): the quantity with constraint (partially screened)
Q. How do we evaluate one-body part ?
A. Maximally localized Wannier function (maxloc)
N. Marzari and D. Vanderbilt, Phys. Rev. B. 56 12847 (1997)
I. Souza et al., ibid. 65, 035109 (2001)

## Slide 7
t1u band
W=0.51eV
Target (T)
Occupied (O)
Virtual (V)
YN-Nakamura-Arita, Phys. Rev. B 85, 155452 (2012)
One body part of the Hamiltonian
Max loc Wannier
Hopping between molecular orbital
Band structure of fcc K3C60

## Slide 8: Ab initio downfolding for electron-phonon coupled systems
Low-energy models for electron-phonon coupled systems:
i,j: orbital (Wannier) indices (w): Wannier gauge s : spin index
O(p): the quantity with constraint (partially screened)
Q. How do we evaluate ?
A. Constrained random phase approximation (cRPA)
F. Aryasetiawan et al., Phys. Rev. B. 70 19514 (2004)

## Slide 9: Constrained RPA
exclude the contribution from
T↔T scattering
This screening process should be considered when we solve the low-energy effective model
・Independent particle polarizability(RPA)
F. Aryasetiawan et al., Phys. Rev. B. 70 19514 (2004)
V:virtual
T:target
EF
T
Occupied (O)
V
①
②
③
④
①
②
③
④
＝①＋②＋③＋④

## Slide 10: cRPA result for C60 superconductors
U～1eV, J～0.035eV
YN-Nakamura-Arita, Phys. Rev. B 85, 155452 (2012)
fcc A3C60
A15 Cs3C60

## Slide 11: cRPA result for C60 superconductors
U～1eV, J～0.035eV, V～0.3eV, and W～0.5eV
Strongly correlated system
Correlation strength (U-V)/W
YN-Nakamura-Arita, Phys. Rev. B 85, 155452 (2012)

## Slide 12: Ab initio downfolding for electron-phonon coupled systems
Low-energy models for electron-phonon coupled systems:
i,j: orbital (Wannier) indices (w): Wannier gauge s : spin index
O(p): the quantity with constraint (partially screened)
Q. How do we evaluate and ?
YN, K. Nakamura, and R. Arita, Phys. Rev. Lett. 112, 027002 (2014)
cf. Density-functional perturbation theory (without constraint)
S. Baroni et al, Rev. Mod. Phys. 73, 515 (2001).
A. Constrained density-functional perturbation theory (cDFPT)

## Slide 13: Phonon frequency and electron-phonon coupling
Phonon frequencies and electron-phonon couplings are given by
(for simplicity we consider the case where there is one atom with mass M in the unit cell)
where
: characteristic
length scale
Dynamical matrix
E : electron ground-state energy
α: cartesian coordinates (x,y,z)
n(r): electron density
bare
Hartree + exchange correlation terms (screening)
ν：phonon mode
u : displacement of the ion
S. Baroni et al, Rev. Mod. Phys. 73, 515 (2001).
Interatomic force constant
(~spring constant)
bare
renormalizing (softening)
Potential change due to the ionic displacement

## Slide 14: Constrained density-functional perturbation theory
Partially screened quantities such as and
In the metallic case, is given by
Exclude target-target processes
n,m: band indices
V:virtual
T:target
EF
T
Occupied (O)
V
①
②
③
④
①
②
③
④
YN, K. Nakamura, and R. Arita, Phys. Rev. Lett. 112, 027002 (2014)
(excluding the target-subspace renormalization effect)
Effective on-site el-el interactions coming from the exchange of phonons:
momentum-space average -> on-site quantity

## Slide 15: cDFPT results for fcc A3C60
 | K3C60 | Rb3C60 | Cs3C60 | Cs3C60 | Cs3C60
Uph (0) [eV] | -0.15 | -0.14 | -0.11 | -0.12 | -0.13
U’ph (0) [eV] | -0.053 | -0.042 | -0.013 | -0.022 | -0.031
Jph (0) [eV] | -0.050 | -0.051 | -0.051 | -0.051 | -0.052
|Jph (0) | ~ 0.05 eV > JH ~ 0.035 eV
(Inverted Hund’s rule)
U’ph ~ Uph – 2Jph
Frequency dependent interaction
frequency dependence
ωl
Uph
ωD ~ 0.1-0.2 eV
-0.15
Lattice constant
large
small
Uph = Vii,ii , U’ph = Vii,jj , Jph = Vij,ij

## Slide 16: Conclusion
developed an ab initio downfolding method for el-ph coupled systems
- applicable also to multi-ferroic materials, thermoelectric material, dielectrics,
polaron problem, …
Results for C60 superconductors
  Effective Coulomb interaction parameters
  U ~ 1 eV, J ~ 0.035 eV → strongly correlated systems
  Effective phonon mediated interaction parameters:
      Uph(0) ~ -0.1 eV, Jph(0) ~ -0.05 eV
  Inverted Hund’s rule is realized
YN, K. Nakamura, and R. Arita, Phys. Rev. Lett. 112, 027002 (2014)
YN-Nakamura-Arita, Phys. Rev. B 85, 155452 (2012)

## Slide 18
改良された連続時間量子モンテカルロ法による
多軌道クラスター動的平均場理論
Multi-orbital cluster dynamical mean-field theory
with an improved continuous-time quantum Monte Carlo algorithm
野村悠祐、酒井志朗、有田亮太郎
東大工
P29

## Slide 19: Dynamical Mean-Field Theory (DMFT)
◎local dynamical quantum correlation
◎can treat el-el and el-ph interaction on same footing
× spatial correlation
Lattice model single-impurity Anderson model
+ self-consistency
map
G. Kotliar and D. Vollhardt, Physics Today, 3, 53 (2004).
Quasi- particles
Upper
Hubbard band
Lower
Hubbard band

## Slide 20: DMFT with quantum Monte Carlo
CT-INT -weak coupling expansion (diagrammatic approach)
  ◎cluster expansion
  ◎can treat various types of interaction (Hund’s coupling, el-ph interaction)
  × low temperature
CT-AUX -weak coupling expansion (auxiliary-field decomposition)
  ◎cluster expansion
  ◎efficient update scheme (submatrix update)
  × low-temperature
  × various types of interaction
CT-HYB -strong coupling expansion
  ◎low temperature (single site DMFT)
  ◎density-type electron-phonon coupling
  × cluster expansion (computational time grows exponentially with the degrees of freedom)
E. Gull et al., Rev. Mod. Phys. 83, 349 (2011)

## Slide 21
CT-INT algorithm①
A. N. Rubtsov et al., Phys. Rev. B 72, 035122 (2005).
F. F. Assaad and T. C. Lang, Phys. Rev. B 76, 035116 (2007).
Action of the single-orbital impurity problem
where we introduce additional parameter
To reduce the sign problem, we rewrite the action as
: Weiss function for the spin σ
: Weiss function with a new chemical potential

## Slide 22: CT-INT algorithm②
We define a configuration and a notation for “sum” over configuration space
A. N. Rubtsov et al., Phys. Rev. B 72, 035122 (2005)
F. F. Assaad and T. C. Lang, Phys. Rev. B 76, 035116 (2007)
Interaction expansion of the partition function leads to
Wick’s theorem
Then the partition function is written as
Weight for configuration Cn

## Slide 23: Fast update scheme
Choose update (insertion or removal)
  Insertion: pick τ （0 ≦ t＜ b） randomly and choose s = ±1
  Removal: choose one of the existing vertices
Compute the ratio of the weight W(C’)/W(C)
Metropolis
  Acceptance ratio:
  Renew configuration if accepted
  Leave old configuration if rejected
Update A-1 (A-1 is used to calculate W(C’)/W(C))
  O(n2) operation
  If configuration is unchanged, A-1 is also unchanged
Go to step 1
E. Gull et al., EPL, 82, 57003 (2008)

## Slide 24: Submatrix update scheme
P. K. V. V. Nukala et al., Phys. Rev. B 80, 195111 (2009).
E. Gull et al., Phys. Rev. B 83, 075122 (2011).
Starting from the initial configuration C0, kmax times updates are done
  Choose update (insertion or removal)
    Insertion: pick τ （0 ≦ t＜ b） randomly and choose s = ±1
    Removal: choose one of the existing vertices
  Compute the ratio of the weight W(Ck’)/W(Ck)
  Metropolis
    Renew configuration if accepted Ck+1 = Ck’
    Leave old configuration if rejected Ck+1 = Ck
  Go to step 1.1
Update A-1 at once after kmax times updates
Go to step 1 with C0(new) = Ckmax
×kmax times
(0 ≦ k ≦ kmax-1)
~ 10 times speed up !

## Slide 25: Extension to multi-orbital systems
i, j: orbital
σ: spin
Action of the multi-orbital impurity problem
We introduce additional parameters
δ2: small positive
number
E. Gorelov et al., Phys. Rev. B 80, 155132 (2009)
reduce sign problem
needed to ensure ergodicity (if [G0]ij = 0)
large δ2 → sign problem

## Slide 26: Efficient sampling of spin-flip and pair-hopping terms
In two-orbital case, weight of a configuration with odd number of J vertices is zero.
We only need to insert/remove two J vertices simultaneously
We do not need to introduce δ2
2D square lattice, t = 1, t’ = 0
two-orbital Hubbard model, half-filling
W = 8t
U = 6.9 t, J= U/6, U’ = U – 2J
T = 0.05 t
single-site DMFT
no symmetry breaking
δ2 = 0.1, norm ~ 53 %
δ2 = 0.05, norm ~ 83 %
δ2 = 0.01, norm ~ 99 %
Number of J vertices

## Slide 27: Results: 2D Hubbard model
2D square lattice, t = 1, t’=0
two-orbital Hubbard model, half-filling
W = 8t, J= U/6, U’ = U – 2J
single-site DMFT and cellular DMFT with 4 site cluster
Paramagnetic and para-orbital solution
Starting the self-consistent loop from metallic solution
Phase diagram
Uc (cluster) < Uc (single site)
Difference between the results with and without spin-flip and pair-hopping terms:
  Cluster DMFT: small
  Single-site DMFT: large
Single-site DMFT
  Entropy(ins,SU(2)) ~ ln(3) (S=1, Sz = 1,0,-1)
  Entropy(ins,Ising) ~ ln(2) (S=1, Sz=±1)
Cluster DMFT
  Entropy(metal) > Entropy(ins)

## Slide 28: Self energy: 2D Hubbard model
(π,0)
(π,π)
(0,0)
・Divergence Im Σπ0
→ Mott transition
・Abrupt change in Re Σ00
at Mott transition
・difference between SU(2)
and Ising results is small

## Slide 29: Conclusion
Implemented efficient update scheme (Submatrix update)
Efficient sampling of spin-flip and pair-hopping terms
Results for 2D two-orbital Hubbard model
  Uc (cluster) < Uc (single site)
  Effect of spin-flip and pair-hopping terms
    Cluster: small ↔ single-site large
  Im Σπ0 diverges in the insulating region
Future perspective
Analysis of the derived model for C60 superconductors
Cluster DMFT study of 3 orbital model with 1/3 filling